Alucobest General Specification

| Testing Items |  |  |  |  | Standards |  | Results |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Unit Weight |  |  |  |  | ASTM D792 |  |  | 3mm=3.7kg/M^2, 4mm=4.5kg/M^2 |  |  |  |  |  |
|  |  |  |  |  |  | (aluminum skin of 0.2mm) |  |  |  |  |
| Outdoor Temperature Resistance |  |  |  |  |  | ASTM D1654 |  |  | No abnormality |  |  |  |  |
| Thermal Expansion |  |  |  |  | ASTM D696 |  |  | 3.0x10^-5.C^-1 |  |  |  |  |
| Thermo Deformation Temperature |  |  |  |  |  | ASTM D648 |  |  | 115 C |  |  |  |
| Thermal Conduction |  |  |  |  | ASTM 976 |  | 0.102kcal/m.hr.C |  |  |  |  |
| Flexural Rigidity |  |  |  |  | ASTM C393 |  |  | 14.0x10^5 |  |  |  |
| Impact Resistance |  |  |  |  | ASTM D732 |  |  | 1650 kgf |  |  |  |
| Adhesive Strength |  |  |  |  | ASTM D903 |  |  | 0.74kgf/mm |  |  |  |  |
| Sound Insulation Rate |  |  |  |  | ASTM E413 |  |  | 29 dB |  |  |  |
| Flexural Elasticity |  |  |  |  | ASTM D790 |  |  | 4055 kgf/mm^2 |  |  |  |  |
| Shear Resistance |  |  |  |  | ASTM D732 |  |  | 2.6kgf/mm^2 |  |  |  |  |
| Minimum Bending Radius |  |  |  |  |  | ASTM D790 |  |  | >= 300mm |  |  |  |
| Wind Pressure Resistance |  |  |  |  |  | ASTM E330 |  |  | Passed |  |  |  |
| Properties Against Water |  |  |  |  |  | ASTM E331 |  |  | Passed |  |  |  |
| Properties Against Air |  |  |  |  | ASTM E283 |  |  | Passed |  |  |  |

Note: The Information Contained herein, to the best of our knowledge is true and accurate, but all recommendations and suggestions are made without guarantee. This information is for use for persons having technical skill and is at their own discretion and risk. Alucobest makes no warranties, express or implied and assume no liability in connection with any use of this information.